COURSE UNIT (MODULE) DESCRIPTION

| Course unit (module) title | Code |
| --- | --- |
| Micro- and Nano-Fabrication Technologies |  |

| Lecturer(s) | Department(s) where the course unit (module) is delivered |
| --- | --- |
| Coordinator: Dr. Mangirdas Malinauskas Other: PhD. Stud. Edvinas Skliutas | Laser Research Center, Faculty of Physics |

| Study cycle | Type of the course unit (module) |
| --- | --- |
| Second (master program) | Compulsory |

| Mode of delivery | Period when the course unit (module) is delivered | Language(s) of instruction |
| --- | --- | --- |
| Auditorium | Autumn semester | Lithuanian |

| Requirements for students |
| --- |
| Prerequisites: Courses of Optics, Laser Physics (or Quantum Electronics) | Additional requirements (if any): |

| Course (module) volume in credits | Total student’s workload | Contact hours | Self-study hours |
| --- | --- | --- | --- |
| 5 | 140 | 48 | 92 |

| Purpose of the course unit (module): programme competences to be developed |
| --- |
| General: training of critical thinking, ability to work in a team with diverse preparation, individual processing and comparison of information. Specific: identify, understand, explain and apply in practice advanced micro- and nano-fabrication technologies; knowledge of fundamentals and operation of diverse techniques , ability to apply them in practice; understanding of modern trends of precision material processing technologies, their widespread worldwide and Lithuania. |
| Learning outcomes of the course unit (module) | Teaching and learning methods | Assessment methods |
| Understanding of nonlinear optical phenomena | Lectures | Exam, presentation on selected topic |
| Training of practical skills, ability to apply nonlinear optical phenomena in practice | Laboratory work | Defence of laboratory work results |

| Content: breakdown of the topics | Contact hours | Self-study work: time and assignments |
| --- | --- | --- |
|  | Lectures | Tutorials | Seminars | Exercises | Laboratory work | Internship/work placement | Contact hours | Self-study hours | Assignments |
| 1. Introduction to photon and charged beam lithographies. Radiation energy, dose, power, intensity, reversable and irreversible impact. Fundamentals of lithography: masks, technological processes, possibilities and limitations. | 2 |  |  |  |  |  | 2 | 4 | Reading of lecture notes, textbooks and scientific literature. |
| 2. Direct laser writing (DLW). Serial laser writing. Surface (2D) and volume (3D) material processing. Additive and subtractive fabrication methods. CAD-CAM production. Linear and non-linear absorption. | 2 |  |  |  | 4 |  | 6 | 12 | Reading of lecture notes and textbooks, preparation for laboratory works. |
| 3. Non-linear/multi-photon lithography (NLL, 2PP/TPP, MPP). Non-linear absorption in volue at tight focusing conditions. Avalanche ionization and thermal accumulation. Polymerization and optical damage thresholds. | 2 |  |  |  | 4 |  | 6 | 12 | Reading of lecture notes and textbooks, preparation for laboratory works. |
| 4. STED, RESOLFT, EUV, light sheet and other advanced light lithography techniques. Optical and chemical quenching of reactions. Excitation-depletion (multi-color), extreme UV, light sheet lithographies. | 2 |  |  |  |  |  | 2 | 4 | Reading of lecture notes, textbooks and scientific literature. |
| 5. Interference/holographic and projection lithographies, digital light processing (DLP). Multi-beam processing of materials: interference and projection exposure. Digital (dynamic) and dual (photo-photo and photo-thermo) exposures. | 2 |  |  |  | 4 |  | 6 | 12 | Reading of lecture notes and textbooks, preparation for laboratory works. |
| 6. Soft-lithography (micro-replication). Micro-stamping and pattern transfer techniques, replications, elastomeric masks, thermopolymers. | 2 |  |  |  | 4 |  | 6 | 12 | Reading of lecture notes and textbooks, preparation for laboratory works. |
| 7. Nanoimprint lithography (NIL). Peculiarities of nanoimprint lithpgraphy and roll-to-roll implementation. | 2 |  |  |  |  |  | 2 | 4 | Reading of lecture notes, textbooks and scientific literature. |
| 8. Nanosphere lithography. Nanosphere (colloid) lithography and self-organisation. Multi-step lithography. | 2 |  |  |  |  |  | 2 | 4 | Reading of lecture notes, textbooks and scientific literature. |
| 9. Electron beam lithography. Fabrication of masks and nano-prototyping using electron beam, advantages and limitation comparing to laser lithography. | 2 |  |  |  |  |  | 2 | 4 | Reading of lecture notes, textbooks and scientific literature. |
| 10. Focussed ion beam machining. Specifics of ion beam, advantages and limitations. Applications and comparison to photon beams. | 2 |  |  |  |  |  | 2 | 4 | Reading of lecture notes, textbooks and scientific literature. |
| 11. Atomic force/thermal proble lithography. Atomic force (contact) and thermal proble lithography. | 2 |  |  |  |  |  | 2 | 4 | Reading of lecture notes, textbooks and scientific literature. |
| 12. Pulsed Laser Ablation in Liquids (PLAL). Material processing in gas and liquid environments, laser assisted nanoparticle generation. | 2 |  |  |  |  |  | 2 | 4 | Reading of lecture notes, textbooks and scientific literature. |
| 13. Laser induced forward transfer (LIFT). Pulsed light radiation induced material transfer. | 2 |  |  |  |  |  | 2 | 4 | Reading of lecture notes, textbooks and scientific literature. |
| 14. Alternative 3D printing options: SLS, SLM, FDM/FFF, InkJet, Binder Jetting. Seletive laser sintering/melting, thermal extrusion deposition, jet printing and binding. | 2 |  |  |  |  |  | 2 | 4 | Reading of lecture notes, textbooks and scientific literature. |
| 15. Hybrid (additive and subtractive) precision material 3D processing. Combination of additive and subtractive laser, electron and ion beam, mask and beam based material processing methods. | 2 |  |  |  |  |  | 2 | 2 | Reading of lecture notes, textbooks and scientific literature. |
| 16. MNFT widespread in Lithuania and worldwide, nowadays made functional structures and future perspectives. The demand of advanced micro- and nano-fabriction technologies in science and their practical applications, significant breakthroughs and trends. | 2 |  |  |  |  |  | 2 | 2 | Reading of lecture notes, textbooks and scientific literature. |
| Total | 32 |  |  |  | 16 |  | 48 | 92 |  |

| Assessment strategy | Weight, % | Deadline | Assessment criteria |
| --- | --- | --- | --- |
| Laboratory work | 20 | By the end of semester | 5 laboratory works, each work is defended separately. The final mark is from 0 to 2, which add to a final course mark. |
| Presentation | 10 | By the end of semester | Presentation on selected topic, answer to questions, brief discussion. Evaluation, which will add up to 1 mark to a final course mark. |
| Exam | 80 | By the end of the course | Exam in written form, 8 questions from the whole course. Answers to each topic are marked as follows: 0 (incorrect/no answer), 0.5 (partially correct) and 1 (correct). All marks sum up. |
| Overall | 100 |  | The overall mark is the sum of the above items and is rounded. <5 below threshold 5 – weak 6 – satisfactory 7 – average 8 – good 9 – very good 10 – excellent |

| Author | Year of publication | Title | Issue of a periodical or volume of a publication | Publishing place and house or web link |
| --- | --- | --- | --- | --- |
| Compulsory reading |
| M. Malinauskas | 2020 | Collection of MNFT presentations |  | Manuscript |
| T. Baldacchini | 2020 | Three-Dimensional Microfabrication Using Two-Photon Polymerization | 2nd. Ed. | Elsevier, 512 p. |
| J. Stampfl, R. Liska, A. Ovsianikov | 2016 | Multiphoton Lithography: Techniques, Materials, and Applications |  | 386 p. |
| Optional reading |
| E. Skliutas, M. Lebedevaitė, E. Kabouraki, T. Baldacchini, J. Ostrauskaitė, M. Vamvakaki, M. Farsari, S. Juodkazis, M. Malinauskas | 2021 | Photopolymerization mechanisms at a patio-temporally ultra-confined light | 10, 1211 | Nanophotonics, De Gruyter, 32 p. |
| S. Varapnickas, M. Malinauskas | 2020 | Processes of Laser Direct Writing 3D Nano-Lithography | Handbook of Laser Micro- and Nano-Engineering | Springer, 31 p. |
| L. Jonušauskas, S. Juodkazis, M. Malinauskas | 2018 | Optical 3D printing: bridging the gaps in the meso-scale | 20, 053001 | Journal of Optics, IOP |
| M. Malinauskas, A. Žukauskas, S. Hasegawa, Y. Hayasaki, V. Mizeikis, R. Buividas, S. Juodkazis | 2016 | Ultrafast laser processing of materials: from science to industry | 5, e16133 | Light: Science and Applications, Nature |
| M. Malinauskas, M. Farsari, A. Piskarskas, S. Juodkazis | 2013 | Ultrafast-laser micro/nano-structuring of photopolymers: a decade of advances | 533, 1 | Physics Reports, Elsevier |
| M. Malinauskas, G. Kiršanskė, S. Rekštytė, T. Jonavičius, E. Kaziulionytė, L. Jonušauskas, A. Žukauskas, R. Gadonas, A. Piskarskas | 2012 | Nanophotonics lithography: a versatile tool for manufacturing functional three-dimensional micro-/nano-objects | 52, 312 | Lithuania Journal of Physic, LPS |